## Slide 1
“Our Science … Your Success”

## Slide 2
  Anaerobics
AA
  Cyanoacrylates
CA
  Two Component Epoxies
ET
  One Component Epoxies
ES
  Structural Acrylics
TA
  Modified Epoxies
MT
  MS Polymers
MS
  Two Component Polyurethanes
PT
  UV Curable
UV
Permabond Product Lines

## Slide 3
Anaerobic Adhesives & Sealants
Single part liquid that cure to a solid plastic at room temperature
Used to secure tight-fitting metal parts
Cures in the presence of metal and absence of oxygen
Description

## Slide 4
Less weight than mechanical locking devices
Easy clean up
Fast
No odor
Chemical and heat resistance
Advantages
Anaerobic Adhesives & Sealants

## Slide 5
Anaerobic Adhesives & Sealants
Threadlocking
Pipe Sealing
Retaining
Gasketing
Products vary in strength, recommended substrates, viscosity, gap fill, temperature resistance and color.
Uses
Notes: Discuss threadlocking blind hole, Retaining = press fit 750 to 2000 psi = retaining compound on machine finish up to 3400 pipesealing Sealants prevent leakage of gases and liquids from threaded pipe joints and fittings. Lock pipes in place Seals to the burst strength of most pipes Prevents corrosion and galling threads Will not contaminate the internal system
Replace Non-curing pipe dopes- Poor solvent resistance No locking effect Solvent-based pipe dopes - Shrink during cure - Fittings must be re-torqued Tapes -Teflon tape lubricates in the off direction-Potential for leaks-Contaminate fluid systemsReduces compression set and fastener loosening
Gasketing Adds structural strength to the assembly Seals all surface imperfections Allows relaxed machine tolerances Eliminates gasket inventories & bolt re-torqueing Single component no mixing - Easy to automate Easier disassembly & clean up than compression gaskets One package can be used for multiple flange sizes Flexible grades available for easy removal

## Slide 6
  Permabond anaerobic numbering consists of two letters followed by three numbers. The letters indicate strength and viscosity, the numbers are unique for each product.
  H = High
  M = Medium
  L = Low
  The first letter represents strength, the second represents viscosity.
    Example: LH050 = Low strength + High viscosity
Product Numbering System
Anaerobic Adhesives & Sealants

## Slide 7
Cyanoacrylates
Single-part adhesives that rapidly polymerize at room temperature
Cure is initiated by moisture on the parts surface. Accelerators available for dry or acidic surfaces
Develop strength extremely fast
Description

## Slide 8
Primary bonding agent.
The adhesive is the only means of holding parts together.
Bonding dissimilar substrates.
Manufacturing aid
Fixturing parts until the next step in the process.
Fingerprint lifter
Fingerprint fuming preserves prints
Uses
Cyanoacrylates

## Slide 9
Humidity
  Low humidity = slower cure speed
Viscosity/Gaps
  Low viscosity for small gaps
Substrates
  PTFE (Teflon®), Silicone, Polyethylene, Polypropylene are difficult to bond and require a primer.
Excess adhesive
  Less is best
  *Teflon is a registered trademarks of E.I. du Pont de Nemours and Company
Factors Affecting Performance
Cyanoacrylates

## Slide 10
Elastomer Bonding
Surface Insensitive
Toughened
High Temperature Resistant
Medical Grades
Metal Bonding
Low Odor
3D Print Infiltrants
Primer and Activators
Cyanoacrylates
Specialty Grades

## Slide 11
Cyanoacrylates
  100 series General purpose plastic bonding, Elastomer EPDM bonding use 105 (except 170)
  800 series High temperature resistance (130°C to 200°C)
  920 series High temperature resistance (250°C after post cure)
  940 series Low odor, Low bloom, Reduces frosting
  2000 series Thixotropic gels, Non-sag, Maximum gap filling
  910 series & 170 Metal bonding
  200 series General purpose plastic bonding
  730 series Toughened, improved impact and peel resistance
  790 series Surface insensitive for acidic surfaces. Extremely fast curing reduces frosting
Notes: Note shear values in the brochure are lap shears of grit blasted steel

## Slide 12
Structural Adhesives are defined as adhesives which can support a structural load when fully cured.
They also provide:
  impact and vibration resistance
  high upper temperature limits
  durable bonds in harsh environments
Description
Structural Adhesives

## Slide 13
Permabond Structural Adhesives
Acrylic External Mix
The two parts fall into each other during dispensing.
Acrylic Bead on Bead
1 Part is dispensed on top of the other part.
Acrylic Surface Activated
Initiator to one surface - Resin to the other surface.
MMA 2-Part
Cure by mixing resin and hardener in correct ratio
Epoxy 2-Part
Cure by mixing resin and hardener in correct ratio
Epoxy 1-Part
Cure with heat in an oven or by infra-red heat

## Slide 14
Description
Epoxies
Permabond epoxies provide structural bonds in a wide variety of applications. One and Two component epoxies are available.

## Slide 15
Two Part Epoxies - ET
Extremely Versatile
Cure Speed
Gap Fill
Temperature & Chemical Resistance
Bond a Wide Variety of Surfaces
Good Impact Resistance
Products available which are
manufactured in compliance with
FDA 175.105 for food
contact applications
Single Part Epoxies – ES
Simple to Use
One Part - No Mixing Required
Very High Performance
Excellent Temperature Resistance
Excellent Chemical Resistance
No Pot Life Limitation
Advantages
Epoxies

## Slide 16
ET5428
Toughened 2-part epoxy
Rapid strength development
Cream colored for GRP/FRP bonding
Available in black for bonding Carbon Fiber
20 – 30 minute handling time
Thixotropic with 0.2” (5mm) gap fill
Lap shear 2900 psi on steel and 3,800 psi FRP Glass/Epoxy
Peel strength >155N/25mm
ET5429
Toughened 2-part epoxy
Black for bonding Carbon Fiber
5 – 6 hours handling time
Thixotropic with 0.2” (5mm) gap fill
Lap shear >2,900 psi on steel and Carbon Fiber Composite
Peel strength >160N/25mm
Excellent temperature performance (435 psi shear strength at 248°F (120°C)
Fast Curing Adhesive For Bonding
Carbon Fiber to Aluminum
ET5428 and ET5429

## Slide 17
MT382
Hybrid 2 part modified epoxy
Highly flexible, Shore A 50
Black for bonding Carbon Fiber
45 minute handling time
Low viscosity, self levelling
Lap shear 1000 psi on steel and Carbon Fiber Composite
Peel strength >120N/25mm
MT3821
60-minute handling time
Thixotropic, gap fill 0.2” (5mm)
Fast Curing Adhesive For Bonding
Carbon Fiber to Aluminum
MT382 and MT3821

## Slide 18
  Permabond’s line of structural acrylic adhesives includes:
          Bead on Bead
          Surface Activated
          Single Part (For metals. Speed can be accelerated with initiator)
          1:1 mixable
  The first three types are ideal for use on metals, magnets, composites, glass, and some thermoplastics. The 1:1 methyl methacrylates are ideal for plastics, metals, and un-primed metals. Permabond TA46xx series is ideal for difficult to bond plastics.
Structural Adhesives are defined as adhesives which can support a structural load when fully cured.
They also provide:
  impact and vibration resistance
  high upper temperature limits
  durable bonds in harsh environments
Description
Structural Acrylic Adhesives

## Slide 19
Advantages
Structural Acrylic Adhesives
  Rapid room temperature cure - no ovens required
  100% solids - Environmentally friendly
  Non stringing – Clean, efficient process
  Thixotropic viscosity –Easy to dispense
  Lower odor – Worker comfort
  Non flammable – (except MMAs) Reduced shipping and handling costs
  High shear strength – Strong
  Toughened - Impact, vibration and peel resistance
  Durable in high moisture environments – Long component life
  High temperature resistance up to 390°F – Design flexibility

## Slide 20
Permabond TA4605 and TA4610 bond untreated polyolefin surfaces. They are ideal for bonding polypropylene, polyethylene, and PTFE without the need for pre-treatment. These Adhesives have much lower odor than MMAs.
Structural Acrylics For Difficult to Bond Plastics
Polyolefins
Above polypropylene lap shears bonded with
TA4610 stretch and deform before the bond fails.

## Slide 21
NEW! Permabond TA4660 is a two-part structural adhesive ideal for bonding filled and unfilled nylon. No primer or surface pretreatment is needed to form bonds that exceed the strength of the nylon. This 2:1 mix ratio, low odor, room temperature curing adhesive also bonds metals.
Structural Acrylics For Difficult to Bond Plastics
Nylon
Above nylon lap shears bonded with TA4660
deform and break before the bond fails.

## Slide 22
Description
Flexible Adhesives
Modified Epoxies, and MS Polymers offer flexibility and provide
unique benefits. Their flexibility combined with low shrinkage make them ideal for bonding thin substrates with no read through and for potting without exerting stress on sensitive components.
Modified Epoxies are two component and MS Polymers are single component room temperature moisture curing.

## Slide 23
Advantages
Flexible Adhesives
Absorb stresses from thermal expansion
Paintable
Non-corrosive
Fast Tack Free Time
Adhesion to a Variety of Substrates
No primer needed
Weather Resistant - No Cracking or Splitting
Ease of Application - Use in Most Weather Conditions

## Slide 24
Description
Polyurethane Adhesives
Two component resin and hardener.
Used for bonding potting and encapsulating.

## Slide 25
Description
UV Curable Adhesives
Single-part adhesives that rapidly polymerize while exposed to UV light.
Permabond has adhesives that cure with UV and Visible light.
A dual cure adhesive/sealant that cures anaerobically as well as with UV light is available for specialty applications.
Dual cure with moisture is also available.

## Slide 26
Factors Affecting Cure
UV Curable Adhesives
Product
Light Intensity
-Distance
- Lamp focal point
- Transmission of light through the substrate.
- Measure intensity at the bond site.
Wavelength
- UV
- Visible
Time

## Slide 27
Top Markets
Industrial Product OEM’s
  Heat Exchangers
  Filter Makers
  Motor Magnet Bonding
  Speaker Makers
  Thread Locking
  Gasket Makers
Aerospace
  Applications to the Lockheed or Boeing specification
Electronics
  Potting
  High temperature bonding
  Carbon Fiber bonding
Difficult / Dissimilar Substrates
  LSE bonding TA46xx
  Metals to Plastics

## Slide 28
Questions…